## Slide 2
MASSACHUSETTS INSTITUTE OF TECHNOLOGY X HONEYBEE ROBOTICS
Co-Leads: Palak B Patel, Jose Soto, Team Members: Zachary K Adams, Derek Chan, Amber Cooper, Jonatan Fontanez, Laman Jalil, Christopher Kwon, Kir Latyshev, Beverly Ma, Lanie McKinney, Cesar Meza, Kristoff Misquitta, Hyein Na, Tom Nguyen, Hezekiah Pendley, Lokesh Sangabattula, Helena Usey, Alice Zehner, Advisors: Lead Advisor: Jeffrey Hoffman, Co-advisors: Antoine Allanore, Martin Culpepper, Olivier de Weck, George Lordos
Notes: Palak

## Slide 3: T E A M M E M B E R S I N A T T E N D A N C E
Jose Soto
Team Lead
Palak Patel
Team Lead
Team Members not attending Forum:
Laman Jalil, Kir Latyshev, Lanie McKinney, Cesar Meza, Hezekiah Pendley
Advisors not attending:
Prof. Antoine Allanore, Prof. Martin Culpepper, Prof. Olivier de Weck, George Lordos
Hyein Na
Characterization and Testing
Lokesh Sangabattula
Characterization and Testing
Amber Cooper
MRE Reactor
Helena Usey
Sonicator
Alice Zehner
Characterization and Testing
Jeffrey Hoffman
Advisor
Chrisopher Kwon
Characterization and Testing
Zachary Adams
MRE Reactor Lead
Kristoff Misquitta
MRE Reactor
Derek Chan
MRE Reactor
Tom Nguyen
MRE Reactor
Beverly Ma
Sonicator
Jonatan Fontanez
Sonicator

## Slide 4: Executive Summary
Extraction of Steel via Electrolysis
Lunar Environment Technology Development
Steel Manufacturing
Characterization & Testing
Pressure Vessel Analysis

## Slide 5: Presentation Roadmap
Molten Regolith Electrolysis
Lunar Environment Technology Development
Steel Characterization and Testing
MRE Reactor Build and Testing
Concluding Thoughts

## Slide 6: Metal Production Pipeline
COLLECTION
BENEFICIATION
ELECTROLYSIS
ALLOYING
STEEL & SLAG COLLECTION
STEEL
MANUFACTURING
PRESSURE VESSEL
OXYGEN VALUE CHAIN
SLAG VALUE STREAM
CAST STEEL PARTS

## Slide 7
COLLECTION
BENEFICIATION
ELECTROLYSIS
ALLOYING
STEEL & SLAG COLLECTION
STEEL
MANUFACTURING
PRESSURE VESSEL
OXYGEN VALUE CHAIN
SLAG VALUE STREAM
CAST STEEL PARTS
ARTEMIS STEELWORKS

## Slide 8: ARTEMIS STEELWORKS
ELECTROLYSIS
STEEL & SLAG COLLECTION
STEEL
MANUFACTURING

## Slide 9: Molten Regolith Electrolysis

## Slide 10: Molten Regolith Electrolysis (MRE) Fundamentals
Hold regolith around 1600°C
Apply voltage, ions migrate according to charge
  Fe2+ ions to cathode (-), O2- to anode (+)
Electron pulled off oxide, forms oxygen
  Electron travels through wire to cathode
Fe2+ reduced to metal at cathode

## Slide 11: MRE Reactor Design

## Slide 12: Simulations and Calculations aided Development
Beneficiation essential
  LHS-1 too low in FeO
Metal composition and thermodynamic voltage calculated
Estimation of power consumption
  100g, ~3x thermodynamic voltage: 7.30kW
The change in composition of the regolith after a theoretical beneficiation step

## Slide 13: Lunar Environment Technology Development

## Slide 14: Lunar Environment Technology
Extraction of Steel in a Vacuum Environment
Extraction of Steel without Beneficiation or Varying Beneficiation
Electrolysis Efficiency Increase for Low Gravity via Sonication
Automation of Steel and Slag Collection
Steel Manufacturing in a Vacuum Environment

## Slide 15: Steel Extraction in Vacuum Environment
Iridium wire with an iron deposit shown via overlayed EDS data

## Slide 16: Steel Extraction at Various Beneficiation Levels
Stacked bar plot showing the composition of different metals produced in small scale testing. The final composition was determined via thermodynamic modelling

## Slide 17: Electrolysis Efficiency Improvement
On the moon, buoyancy force is reduced to 1/6th.
Consequently, the bubbles could expand and take longer to detach from the anode, inhibiting the electrolysis reaction and shortening the lifespan of the electrodes due to corrosion.
We incorporated a sonicator on the anode to induce vibrations that detach the bubbles while they are still small.

## Slide 18: SIS+ER to Demonstrate Automation
ARTEMIS Steelworks incorporates a Slag-and-Iron-Slicer (SIS) and (+) Extraction Rod (ER) setup.
The ER pulls out the electrolysis products.
The SIS will then saw through the resultant iron and slag for collection.
Back Rod Opposer (BRO) used to mitigate shear forces on motor.

## Slide 19: Automation Tests
SIS+ER low risk tests.
  Created a SIS+ER test mount.
Attached a cast iron rod
  Pure Fe Hardness (Vickers Scale): 150
  Pure Cast Iron Hardness (Vickers Scale): 246
ER actuated and tested resistance against cutting test.
Video of our SIS in action
Video of our ER in action
SIS+ER Testing Mount

## Slide 20: Steel Manufacturing in Vacuum Environment
Mixing Steel Simulant by Reheating
Casting with Liquid Cooling
Polishing Samples
Grain Imaging and Hardness Testing
Arc Melting in a Vacuum Environment
___
1cm
Titanium
Iron
Silicon

## Slide 21: Steel Manufacturing in Vacuum Environment
Mixing Steel Simulant by Reheating
Casting with Liquid Cooling
Polishing Samples
Grain Imaging and Hardness Testing
Suction Casting in a Vacuum Environment
TOM REMEMBER TO ADD THIS VIDEO :3

## Slide 22: Steel Manufacturing in Vacuum Environment
Mixing Steel Simulant by Reheating
Casting with Liquid Cooling
Polishing Samples
Grain Imaging and Hardness Testing
Polishing samples for testing
SST-1, Slow cooled
SST-1, Fast cooled
SST-2, Slow cooled
SST-2, Fast cooled

## Slide 23: Steel Manufacturing in Vacuum Environment
Mixing Steel Simulant by Reheating
Casting with Liquid Cooling
Polishing Samples
Grain Imaging and Hardness Testing
Hardness testing
Test Parameters:
Load: 10kgf = 98 N
5 Indentations per sample
Inert Environment

## Slide 24: Steel Characterization and Testing

## Slide 25: Steel Characterization and Testing
Hardness
Yield Strength
YS (MPa) = HV/2.596
Sample​ | Composition​
SST-1​ | 73Fe-20Si-7Ti​
SST-2​ | 52Fe-2Si-46Ti​
SST-2, Fast cooled
SST-2 , Slow cooled
SST-1, Fast cooled
SST-1, Slow cooled
100 µm
100 µm
100 µm
100 µm
Notes: Average Yield Strength across all samples: 225 – 360 MPa
Average Vickers Hardness across all samples: 570 – 820 HV
scale: 200 um each
Micrographs explaining the reason for hardness:
Slag characterization
Metal mfg and strength results etc. Yay lunar steel from MRE reactor!
  Manufactured metal simulant of two composition : SST-1 (73Fe-20Si-7Ti) and SST-2 (52Fe-2Si-46Ti)
  Both simulants were subjected to two different cooling rates : slow cooling and fast cooling
  Characterized the mechanical property (hardness) using Vickers hardness test and observed the microstructure through optical microscopy
  Yield strength was evaluated by typical Tabor factor which will eventually have the same trend as hardness
  The hardness of SST-1 was higher than that of SST-2
  The effect of cooling rate was obvious in SST-1 that faster cooling rate increased its hardness while it was unclear in SST-2
  Microstructure of SST-1 supports the hardness difference due to different cooling rate

## Slide 26: Pressure Vessel Analysis
Using cylinder design with hemisphere ends
Habitat pressure difference = 101,325 Pa
Factor of safety = 2
Notes: Using cylinder design with hemisphere ends
Ambient pressure = to Earths, 101325 Pa
Factor of safety = 2
To get the largest vessel for smallest amount of metal, results show unenriched, fast cooled regolith was better [diameter 7m and thickness of 0.0098 m or diameter of 12 m and thickness 0.0017 m]
Study done with habitats in mind, could also be produced for fuel storage

## Slide 27: MRE Reactor Build and Testing

## Slide 28: Building the MRE Reactor
Prof. Allanore's lab at MIT
~10 students
~ 200 hours per person

## Slide 29: Subsystem Verification Testing
Argon Gas Leak Test

## Slide 30: Subsystem Verification Testing
Heating Element Test

## Slide 31: Subsystem Verification Testing
Endcap Cooling Water Leak Test

## Slide 32: MRE Reactor Process

## Slide 33: System Verification Testing
Step 1: Place regolith inside tube

## Slide 34: System Verification Testing
Step 2: Vacuum and purge with Argon

## Slide 35: System Verification Testing
Step 3: Turn the furnace on

## Slide 36: System Verification Testing
The system is running!

## Slide 37: System Verification Testing
Old heating elements (couldn't be replaced due to lead time) and low insulation led to inability to reach operation temperature of 1550°C
Bubbles
Broken Inner tube
Molten regolith

## Slide 38: Concluding Thoughts

## Slide 39: Conclusion
Extraction of Steel via Electrolysis

## Slide 40: Conclusion
Extraction of Steel via Electrolysis
Lunar Environment Technology Development
Extraction of Steel in a Vacuum Environment
Extraction of Steel without Beneficiation or Varying Beneficiation
Electrolysis Efficiency Increase for Low Gravity via Sonication
Automation of Steel and Slag Collection
Steel Manufacturing in a Vacuum Environment

## Slide 41: Conclusion
Extraction of Steel via Electrolysis
Lunar Environment Technology Development
Steel Manufacturing

## Slide 42: Conclusion
Extraction of Steel via Electrolysis
Lunar Environment Technology Development
Steel Manufacturing
Characterization & Testing

## Slide 43: Conclusion
Extraction of Steel via Electrolysis
Lunar Environment Technology Development
Steel Manufacturing
Characterization & Testing
Pressure Vessel Analysis

## Slide 44: Path to Flight
Required System Capability | Analysis Required | Test Plan
1/6 Gravity | Sonicator Tests in 1/6 Gravity | Sonicator Parabolic Flight Tests
Full Automation Integration | Automated Inlet and Outlet | Hopper and Magnetic Extractor Design
Vacuum Temperature Regulation | Design + Verification Testing for vacuum operation | Thermal Vacuum Testing + Temperature Mitigation Design
Dust Resistance | SIS+ER verification testing w/ dust deposition | Long-term SIS+ER testing with lunar dust + saw particles generation
Long Term Sustainability | ARTEMIS Steelworks Longevity verification | Tests proving long-term operational capability

## Slide 45: Future Work
Run the reactor with new heating elements and beneficiation
Test the reactor with the sonicator to see the improvement in efficiency
Test the reactor in a TVAC
Steel manufacturing with hot rolling and cold rolling
Test steel in tensile testing

## Slide 46
Thank you for your attention