## Slide 2
Lunar In-Situ Aluminum Production through Molten Salt Electrolysis (LISAP-MSE)
J. N. Ortega, J. Smith, F. Rezaei, D. Bayless, W. Schonberg, D. Stutts, and D. Han (handao@mst.edu)
Missouri University of Science and Technology, Rolla, MO 65409
Undergrad Team Members:

## Slide 3: Outline
Motivation
Background
LISAP-MSE Method Overview
LISAP-MSE Phase 1
LISAP-MSE Phase 2
Conclusions
Future Work

## Slide 4: Motivation
Artemis Base Camp (ABC)
Additive Manufacturing
100% ISRU
Source: ICON/SEArch+

## Slide 5: Terrestrial Methods
Current State of the Art Bauxite (Al2O(OH)) Sodium aluminate (NaAlO2) Aluminum hydroxide (Al(OH)3) Alumina (Al2O3) Cryolite (Na3AlF6)

## Slide 6: FFC Cambridge Method
Starting Point
Tested for Many Metallic Oxides
Chen et. al., 2013 [1]
Kilby et. al., 2006 [2]

## Slide 7: LISAP-MSE Method
Adapted from Kadowaki et. al., 2018 [3]
Phase 2
Phase 1

## Slide 8: Leaching & Thermal Reduction Process (LISAP-MSE Phase 1)

## Slide 9: Leaching Characterization Data (Success)
7% Ca by Mass
Chart: 
| Alumina | Calcium Aluminate (Hibonite)* | Calcium Aluminate (Grossite)**
Mass Percent | 37 | 35 | 28
35 %
* Hibonite: CaAl12O19
** Grossite: CaAl4O7

## Slide 10: Electro-deoxidation Process (LISAP-MSE Phase 2)
Design validation
Test runs
Alternate test setups

## Slide 11: Basin Design & Heat Test

## Slide 12: Heat Test Result

## Slide 13: Furnace Testing

## Slide 14: Furnace Testing Aftermath

## Slide 15: Furnace Testing Results (Unsuccessful)
Chart: 
| Alumina | Calcium Carbonate
Mass Percent | 93 | 7
7 %

## Slide 16: Graphite Cell Test Setup

## Slide 17: Graphite Cell Testing

## Slide 18: Graphite Cell Results (Unsuccessful)
Chart: 
| Alumina | Calcite | Calcium Aluminate | Graphite
Mass Percent | 72.3 | 9.9 | 11.9 | 5.9
5.9%

## Slide 19: Conclusions
Phase 1 Successful but Not Optimized
Phase 2 Needs Work (Some Funds Remaining)

## Slide 20: Future Work
Optimizing the Leaching Process
Redesign of Electrolysis Setup

## Slide 21: Acknowledgements
NASA BIG Idea Challenge 2023
Missouri S&T’s Kummer Innovation and Entruepreneural Fellowship
Missouri Space Grant Consortium
Dr’s Daoru Han, Jeffrey Smith, Fateme Rezaei, David Bayless, William Schonberg, and Daniel Stutts
Todd Sanders and Many Undergraduate Researchers

## Slide 22: References
G. Z. Chen. The FFC Cambridge Process for Metal Production: Principle, Practice, and Prospect. In Proceedings of the Third International Slag Valorisation Symposium, March 2013.
K. C. T. Kilby, L. Centeno, G. Doughty, S. Mucklejohn, and D. Fray. The Electrochemical Production of Oxygen and Metal via the FFC-Cambridge Process. Space Resources Roundtable, 8:64–65, 01 2006
H. Kadowaki, Y. Katasho, K. Yasuda, and T. Nohira. Electrolytic Reduction of Solid Al2O3 to Liquid Al in Molten CaCl2. Journal of The Electrochemical Society, 165(2), 2018.

## Slide 23: Questions?