## Slide 3
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
State of the Art: Polymer-Based Inflatables
  Maximizes deployed-to-stowed volume
  Minimizes mass
  Low SWaP technology
    Habitats
    Towers
    Transportation
    Shielding

## Slide 4
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Polymer Inflatables Unsuitable for Harsh Lunar Conditions
Lunar Dust Abrasion
Space/Solar Irradiation Embrittlement
Temperature Extremes, Fluctuations, Sun-Side Heating
Micrometeorite Damage
Grier et al.
ISS Micrometeorite Damage
   Extremely low repairability, catastrophic failure
   Embrittlement at low temperatures & fluctuating performance
 Punctures, broken filaments
Degradation, premature failure
Breaking of covalent bonds
NASA
NASA
NASA
NASA
NASA
Jean-Pierre Maillard

## Slide 5
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Metal Provides Superior Resilience in the Lunar Environment
Abrasion Resistance
Large Operating Temperature Range
Radiation Resistance
High Repairability/No Critical Failure
SpaceX
DOE
Kennametal

## Slide 6
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
METALS Overview – Difference From Conventional Inflatables
Depressurization or punctures cause catastrophic failure in polymer inflatables
Plastic deformation permanently deploys metal inflatables, even if gas is lost or recovered

## Slide 7
How to Make a Metal Inflatable?

## Slide 8
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
METALS Overview – Simple Manufacturing Process
Shape is cut out from sheet metal (waterjet or laser)
Edges and valves are welded
2D shape is inflated with air or other fluid
Handsome team member
Notes: So now you might be wondering, ubt how you do make a metal inflatable? Well, the process is actually very simple, [simple enough for a undergrad like myself to figure out].
First off, the inflatable geometry is waterjet-cut from sheet metal.
Then, the inflation valve is butt-welded on, followed by edge welding to connect two sheet metal pieces together.
Finally, this 2D shape is pressurized via an air compressor or pressure washer, inflating modules to their 3-dimensional deployed state

## Slide 9
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
The Final Step: Metal Inflation!
48 in. Diameter

## Slide 10
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
METALS Overview – Simple Manufacturing Process
Rapid optimization, scalability,
and flight qualification
Simplicity in manufacturing makes METALS a near-term, high value solution relevant for Artemis missions within this decade.
Simple, reliable, proven manufacturing process
Accelerated
Production Times
Reduced
Fabrication Costs
Accessible Entrance by Commercial Suppliers
Notes: the simplicity of METALS’ manufacturing method stands in contrast to the complex, highly-specialized manufacturing of traditional polymer-based inflatables, thus enabling METALS to achieve accelerated production times, reduced fabrication costs, and accessible entrance by a plethora of commercial suppliers. These benefits streamline the further scaling, optimization, and flight qualification of metal inflatable technologies, making METALS a near-term, high value solution relevant for Artemis missions within this decade.

## Slide 11
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Application: Cryogenic Storage
A sustained human lunar presence requires extensive fluid storage capabilities (especially for cryogenics) with two design criteria:
Metal inflatables are the inevitable solution for the Artemis requirement for scalable cryogenic storage
1.
Scalable deployed storage capacity from compact stowed configuration
2.
Material that retains toughness at cryogenic temperatures
Rigid metal tanks❌
Inflatables✅
Polymers❌
Metals✅
Notes:   Oxygen for life support, propellant
  Methane for propellant
and no metal- or composite-based fluid storage tanks have been designed to be inflatable/deployable.
Traditional polymer-based inflatables lose their toughness at cryogenic temperatures
Thus, the transport of fixed-shape, rigid tanks constitutes the current SOTA in lunar cryogenic storage  inherently volume-prohibitive
a material class suitable for pressurization at cryogenic temperatures + an inflation capability that enables scalable deployed storage capacity

## Slide 12
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Mission Scenario
Flat METALS modules densely stacked within payload volume of lunar lander.
Off load from lander.
Inflate with gas under direct sunlight.
  Increased ductility and toughness during inflation.
  Inflation gas can be heated to amplify this effect.
Gas is recovered and used to inflate other modules.
Packaging and Deployment

## Slide 13
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Mission Scenario
1. Lower into hole from autonomous excavator
2. Connect to fluid distribution network
3. Bury under regolith, fill with fluid
Abundant regolith provides:
Protection from day-night fluctuations
Radiation/micrometeorite protection
Exceptionally thermal insulation
…all with zero payload mass penalty.
Notes: Deployed (but empty) module is then lowered into a hole
Connected via piping to cryogenic fluid distribution network
Buried under regolith and filled with cryogenic fluid
Key benefits of burying:
1. Damps periodic temperature fluctuations of day-night cycle
2. Protection from micrometeorites/radiation (just increase depth until desired safety is achieved!)
3. Exceptional thermal insulation performance for long-term cryogenic storage with minimal energy input

## Slide 14
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Design and Optimization
Variables Defining METALS Design Space
Inflation Pressure,
Alloy Selection
Sheet Metal Thickness,
2D Shape Cut From Stock Sheet Metal
Optimized design will maximize KPP: m3 of fluid storage per kg of sheet metal
Maximize burst pressure for optimal reliability

## Slide 15
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Design and Optimization
Credit to Liam Warlick
Optimized Shape:
Sinusoidal Edged Circle (SEC)
radial distance (r), angle (base radius (R), amplitude (A), and frequency (F)
Discovered thin metal buckles as it’s inflated.
Determined buckling must be controlled.
Carefully designed waves on the edge can ‘guide’ the buckling.
Optimized shape reliably inflates.
Notes: MAXIMIZE VOLUME AND MINIMIZE STRESS

## Slide 16
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Selection of Burying Depth
Dampened Temperature Fluctuations
At 40 cm depth, temperature fluctuations are under 10 K
Limits exposure to high daytime temperatures
Weight of Regolith on Inflatable
Pressure of regolith will counteract pressure of fluid, reducing stress on the inflatable as depth increases.
Weight of regolith is a non-factor (~0.12 PSI per foot of depth).
Internal Pressure
Regolith Pressure
Malla et. al
Notes: At a depth of 40cm into the lunar surface, thermal fluctuations dampen to less than 10 degrees Kelvin, limiting exposure to high daytime temperatures and making temperature-control more manageable.
The proposed burying depth for METALS inflatables at at a minimum depth of 40 cm under regolith layer. This is intended for exemplary radiation shielding, micrometeorite protection, and thermal insulation without any mass penalty of transporting additional material to the Moon.

## Slide 17
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Regolith Thermal Performance
Experimental Setbacks
Variables were difficult and expensive to control
  Initial temperatures, in vacuum, accurate to mission scenario
Preference for Simulation
Offers greater control over realistic parameters of the mission scenario.
Modeled for worst case scenario:
  Constant sunlight
  Perfect regolith solar absorptivity
  Minimum expected fluid storage temperature (70K)
Improved Experimental Setup
Dusty thermal vacuum chamber
Connected cryocooler to achieve steady-state system
Temperature data collection from thermocouples
Attempted Experiment
Bury low-temperature inflatable under regolith
Measure temperature vs time to characterize heat transfer
Notes: A physical experiment was initially pursued for characterizing thermal performance of cryogenic METALS modules, as seen on the right. However, it was determined that controlling initial temperatures and applying a vacuum in a test environment compatible with lunar regolith was not within the budget, and our yielded results did not hold significant meaning to the mission scenario.
An improved experimental setup accurate to mission scenario was determined for potential future research, which would take place in a dusty thermal vacuum chamber. A connected cryocooler would maintain cryogenic temperatures within the module, with thermocouples to record temperature over time.
Due to the difficulty and high-cost of this proposed experiment, a thermal model created using finite element analysis was pursued. This allowed us to model the worst-case mission scenario accurately, considering constant sunlight, perfect regolith solar absorptivity, and the minimum expected fluid storage temperature of 70K.

## Slide 18
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Regolith Thermal Performance
(Kelvin)
2D FEM Thermal Model
Lunar surface absorbing solar flux
Notes: This Ansys Mechanical model simulates an inflatable structure buried under regolith, representing a scenario with high thermal gradients due to direct solar heating at the lunar surface. The model’s two-dimensional axisymmetric geometry centers on an ellipsoidal shape representing a buried inflatable. The top of the model receives a solar flux accurate to 85 degrees latitude, the approximate region where the Artemis base will reside. The temperature field is color-coded on the simulation results, shown in Kelvin.

## Slide 19
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Regolith Thermal Performance – Simulation Results
Stores liquid oxygen for <2 W/m3 (depth of 0.45 m, diameter of 4 m)
Starship HLS capacity (1052.6 m3) for <2100 W
Burying METALS modules at least 0.45 meters is more than sufficient to insulate cryogenic fluid
Increasing depth reduces cooling requirement
Cooling Required for Inflatable Versus Depth
Larger tanks reduce specific cooling requirement ()
Specific Cooling Required Versus Depth
Notes: By solving for steady-state heat transfer, the model showed Burying depths of at least 0.45 meters and inflatables of manufactured diameter of at least 4 meters can maintain cryogenic temperatures for no more than 2 W per cubic meter of liquid oxygen storage. This value is sufficient for storing the entire propellant capacity of Starship HLS (1052.6 m3) for just 2105 Watts. These results confirm that regolith is a highly effective insulator, reducing energy consumption and ensuring long-term, sustainable cryogenic storage.

## Slide 20
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Alternative Approaches for Temperature Control
Permanently Shadowed Regions (Heating)
Aluminized Mylar Shading
Simple, reliable resistive heating
Solid storage when fluid is not in use
Increases storage density
Reduces energy consumption
https://www.lpi.usra.edu/lunar/lunar-south-pole-atlas/
Placed on surface above buried modules
Reduces absorption of solar energy and resulting regolith temperatures
Solution for above ground storage as well
https://science.nasa.gov/mission/cassini/thermal-blankets/
Notes: Further methods for feasible cryogenic storage have been identified to add flexibility of the METALS mission scenario, but must be simulated or experimented in order to quantify thermal benefits, energy consumption, and cost. In conjunction with burying under regolith, a light-weight “tarp” shade of low-emissivity material (such as aluminized Mylar, 0.044) can be constructed above buried modules to block regolith absorption of solar flux, significantly reducing regolith temperatures by up to 60K [10], and thus the rate of heat transfer.
Within Permanently Shadowed Region (PSR) mean temperature of 18K, thermal management becomes an issue of heating, not cooling. This will be safely and reliably accomplished with resistive heating directly in contact with the module. Alternatively, liquid fuel can be pumped to the surface with reasonable efficiency since some energy is recovered on the way down. Additionally, fluid can be stored solid to increase storage density and reduce energy consumption, as heating is only necessary when fluid is to be transferred. This particular mission scenario may be especially energy efficient as continuous energy expenditure is not needed to maintain storage.
(While potentially more logistically challenging to construct/install, storage in a PSR represents the most optimal storage scenario. Active heating is simpler and more reliable, and a loss of power results in solidification, not gasification and loss of stored fluids)

## Slide 21
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Our testing plan (TRL4-TRL5 readiness)
Study the scalability laws of the metal inflatable design through rapid manufacture and iteration,
Evaluate the reliability of the proposed manufacturing methods through repeatable testing campaigns
Evaluate the inflatable design within a variety of relevant lunar conditions to advance its flight-readiness to TRL 5 status.
Standardized inflation pressure
Deformation as a function of pressure
Inflation under vacuum conditions
Cryogenic storage feasibility
Micrometeorite impact resistance
Reliability of welds
Strength testing
Effect of annealing on carbon steel

## Slide 22: Testing & Capabilities
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures

## Slide 23
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Standardized Inflation Pressure
Design Parameters
Geometries: Pentagon, Hexagon, SEC.
Size: 12’’ diameter.
Thickness: 1mm.
Material: Stainless Steel 304.
Overview
Validate the reliability and consistency of three module geometries.
Pressures < 150psi: Submerge modules in water and inflate with air compressor to measure water displacement.
Pressures > 150psi: Inflate with pressure washer, then measure volume by weighting the module with water.
Volume Measurement Methods
Fifteen Modules utilized for SPI Testing, Pre-Inflation

## Slide 24
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Standardized Inflation Pressure
Five Inflated and Burst Octagons
Five Inflated and Burst Pentagons

## Slide 25
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Standardized Inflation Pressure
Five Inflated and Burst Octagon Modules
Five Inflated and Burst Pentagon Modules

## Slide 26
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Standardized Inflation Pressure
Air Compressor Limit
SEC Results
Continuous deformation.
High initial slope before 50 psi.
Plateaus at 50psi, achieving max volume.
Withstands pressures ~10 times bigger than that of octagon and pentagon geometries.
No buckling.
Five Inflated and Burst SEC Modules

## Slide 27
Overview
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Analyze relationship between module deformation and inflation pressure across design parameters.
Design Parameters
Thicknesses: 1mm, 2mm.
Materials: Stainless Steel 304, Low-Carbon Steel 1008.
Geometries: Pentagon, Octagon, Hexagon, SEC.
Deformation vs. Pressure
Top – Deformation vs. Pressure Modules Pre-Inflation.
Bottom – Deformation vs. Pressure Modules Post-Inflation.

## Slide 28
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
1mm = 2mm =
Thickness Selection
Analyze relationship between module deformation and inflation pressure based on material thickness.
Deformation vs. Pressure
Deformation vs. Pressure of Stainless Steel Modules
Deformation vs. Pressure of Low-Carbon Steel Modules

## Slide 29
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
1mm = 2mm =
Thickness Selection
Analyze relationship between module deformation and inflation pressure based on material thickness.
Deformation vs. Pressure
Deformation vs. Pressure of Stainless Steel Modules
Deformation vs. Pressure of Low-Carbon Steel Modules
1mm Performance:
Bigger expansion, lower burst pressures.

## Slide 30
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
1mm = 2mm =
Thickness Selection
Analyze relationship between module deformation and inflation pressure based on material thickness.
Deformation vs. Pressure
Deformation vs. Pressure of Low-Carbon Steel Modules
Deformation vs. Pressure of Stainless Steel Modules
2mm Performance:
Lower expansion, higher burst pressures.
1mm Performance:
Bigger expansion, lower burst pressures.

## Slide 31
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
1mm = 2mm =
Thickness Selection
Analyze relationship between module deformation and inflation pressure based on material thickness.
Deformation vs. Pressure
2mm Performance:
Lower expansion, higher burst pressures.
1mm Performance:
Bigger expansion, lower burst pressures.
↑ Thickness = ↓ Expansion = ↑ Burst Pressure
Deformation vs. Pressure of Stainless Steel Modules
Deformation vs. Pressure of Low-Carbon Steel Modules

## Slide 32
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
1mm = 2mm =
Thickness Selection
Analyze relationship between module deformation and inflation pressure based on material thickness.
Deformation vs. Pressure
Deformation vs. Pressure of Low-Carbon Steel Modules
Deformation vs. Pressure of Stainless Steel Modules
2mm Performance:
Lower expansion, higher burst pressures.
1mm Performance:
Bigger expansion, lower burst pressures.
↑ Thickness = ↓ Expansion = ↑ Burst Pressures
SEC Performance:
Bigger expansion, bigger burst pressures.

## Slide 33
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Material | Shape | Thickness (mm) | Final Volume (mL) | Burst Pressure (psi)
Low-Carbon Steel | SEC | 1 | 4538 | 273
Low-Carbon Steel | SEC | 2 | 5447 | 417
Stainless Steel | SEC | 1 | 4644 | 440
Stainless Steel | SEC | 2 | 5450 | 616
Deformation vs. Pressure
Material Selection
Analyze relationship between module deformation, weld reliability and inflation pressure based on material selection.

## Slide 34
Material Selection
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Deformation vs. Pressure
Analyze relationship between module deformation, weld reliability and inflation pressure based on material selection.
Geometry Selection
Analyze relationship between module deformation and inflation pressure based on geometry selection.
Chart: Inflation Pressure (psi)
Pentagon: ↑ Expansion = ↓ Burst Pressures
Average Deformation vs. Pressure of All 1mm-Thick, Stainless-Steel Modules
Material | Shape | Thickness (mm) | Final Volume (mL) | Burst Pressure (psi)
Low-Carbon Steel | SEC | 1 | 4538 | 273
Low-Carbon Steel | SEC | 2 | 5447 | 417
Stainless Steel | SEC | 1 | 4644 | 440
Stainless Steel | SEC | 2 | 5450 | 616

## Slide 35
Material Selection
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Deformation vs. Pressure
Analyze relationship between module deformation, weld reliability and inflation pressure based on material selection.
Geometry Selection
Analyze relationship between module deformation and inflation pressure based on geometry selection.
Chart: Inflation Pressure (psi)
Pentagon: ↑ Expansion = ↓ Burst Pressures
Octagon: ↓ Expansion = ↑ Burst Pressures
Average Deformation vs. Pressure of All 1mm-Thick, Stainless-Steel Modules
Material | Shape | Thickness (mm) | Final Volume (mL) | Burst Pressure (psi)
Low-Carbon Steel | SEC | 1 | 4538 | 273
Low-Carbon Steel | SEC | 2 | 5447 | 417
Stainless Steel | SEC | 1 | 4644 | 440
Stainless Steel | SEC | 2 | 5450 | 616

## Slide 36
Material Selection
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Deformation vs. Pressure
Analyze relationship between module deformation, weld reliability and inflation pressure based on material selection.
Geometry Selection
Analyze relationship between module deformation and inflation pressure based on geometry selection.
Chart: Inflation Pressure (psi)
Pentagon: ↑ Expansion = ↓ Burst Pressures
Octagon: ↓ Expansion = ↑ Burst Pressures
SEC: ↓ Expansion = ↑ ↑ Burst Pressures
Average Deformation vs. Pressure of All 1mm-Thick, Stainless-Steel Modules
Material | Shape | Thickness (mm) | Final Volume (mL) | Burst Pressure (psi)
Low-Carbon Steel | SEC | 1 | 4538 | 273
Low-Carbon Steel | SEC | 2 | 5447 | 417
Stainless Steel | SEC | 1 | 4644 | 440
Stainless Steel | SEC | 2 | 5450 | 616

## Slide 37
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Vacuum Pressure
Vacuum test 1 – SEC 6 in diameter. 40 psi, 0.05 Torr

## Slide 38
Figures:
Top – Test 2 data, 0.05 Torr, 6 in SEC
Bottom – vacuum test inflatable (left) vs atm pressure inflatable
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Vacuum Pressure
Overview
Evaluate deformation and operational reliability under vacuum pressures.
Setup
VIM2000 vacuum furnace.
Argon tank.
Pressure Transducer.
Yor-Lok fittings.
Results
Same inflation performance.
Final geometry as atmospheric, no ruptures.
1mm SS304 SEC

## Slide 39
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Holding Pressure
Pressurized Pentagon for
Holding Pressure Testing
Overview
Validate pressure-holding capabilities.
Modules
Geometries: SEC and Pentagon.
Thickness: 1mm.
Material: Stainless Steel.
Results
METALS modules can effectively hold pressure when properly sealed.
Method
Pressurize to 22 psi.
Daily pressure checks.
Duration of 14 days.
Pressurized SEC for
Holding Pressure Testing

## Slide 40
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Cryogenic Temperatures
Overview
Evaluate module reliability under cryogenic conditions.
Setup
Modules: 3 x 7’’ SECs (1mm SS 304).
Temperatures: 103K, 171K, 280K.
Pressure: 85 psi.
Assess the effect of cryogenic temperatures on volumetric expansion and material characteristics of inflatables.
Experiment 1
Method
Measurement of final height and RT nano-indentation.
↓ Temperature = ↓ Expansion = ↓ Burst Pressures ≠ Hardness Change
Results
Hardness of each inflatable measured at room temp
Initial Temperature vs. Final Inflation Height

## Slide 41
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Cryogenic Testing Results
Setup
Modules: 2 x 7’’ SECs (1mm SS 304).
Temperatures: inflated at 280K, one cooled to 171K at 85 psi.
Assess the effect of cooling after inflation on failure points.
Experiment 2
Method
Initial Pressurization: 85 psi.
Cooling of one module to 171K.
Final pressurization: 150 psi.
Cooling after Inflation = ↓ Expansion ≠ Failure Pressure
Results
Figure – Burst SEC Module during Cryogenic Temperature Testing Experiment 1
Table – Initial temperature vs. inflation Height of 2 Modules

## Slide 42
Conclusion:
Room temperature pre-inflated module robust for pressurized cryogenics and unlikely to fail
More ductile metals will deform around the weld interface as opposed to cracking
Ideal inflation time/location is in direct sunlight
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Cryogenic Testing Results
Weld pocket ~2 microns
Weld Pocket ~50 microns
Pre inflation
Post-inflation
Change in weld geometry post-inflation in annealed carbon steel

## Slide 43
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Cryogenic Testing Results
Final image of cryogenic inflatable demonstrating much sharper interface
Conclusion:
Room temperature pre-inflated module robust for pressurized cryogenics and unlikely to fail
More ductile metals will deform around the weld interface as opposed to cracking
Ideal inflation time/location is in direct sunlight

## Slide 44
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Repairability
Overview
Develop and test solutions for patching punctures on inflated modules.
Solid-State Solution
TIG welding a 1x1-inch stainless steel patch over a 0.223" puncture
Liquid-State Solution
MIG welding in a spiral pattern
Solid-State Solution Testing
Liquid-State Solution Testing

## Slide 45
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Standard Side Views of Volume Rendering of Samples 1, 2, and 3
Samples 1
Samples 2
Samples 3
Reliability of Welds
Objective
Assess weld reliability to detect internal defects impacting structural integrity.
Method
X-ray micro-computed tomography (microCT) with SkyScan 1276 microCT.
Samples
Materials: 3 samples of Carbon Steel 1008 & Stainless Steel 304 each.
Dimensions: <72mm diameter, <300mm length (for microCT compatibility).
Resolution: 6 µm with 12 mm diameter sample holder.

## Slide 46
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Reliability of Welds
Objective
Assess weld reliability to detect internal defects impacting structural integrity.
Method
X-ray micro-computed tomography (microCT) with SkyScan 1276 microCT.
Samples
Materials: 3 samples of Carbon Steel 1008 & Stainless Steel 304 each.
Dimensions: <72mm diameter, <300mm length (for microCT compatibility).
Resolution: 6 µm with 12 mm diameter sample holder.
Scanning Process
Equipment: SkyScan 1276 microCT for high-precision imaging.
Set-up: full 360° rotation with X-ray tube and detector around the sample.
Time per scan: approximately 5 minutes per sample.
Standard Side Views of Volume Rendering of Samples 1, 2, and 3
Samples 1
Samples 2
Samples 3

## Slide 47
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Sample 1 Slice Views of Volume Rendering of Porosity Defect
High Exposure Side Slice Vie
Low Exposure Side Slive View
Double Slive Orthogonal View
Reliability of Welds
Image Analysis with Amira Software
  Defect Detection: Isolation of internal defects (e.g., cracks, porosity) within welds.
  3D Dataset Alignment: Comparative analysis across samples.
  Visualization: High-resolution 3D renderings to assess defect distribution.
Results
  Sample 1: Porosity defect at the metal joint due to trapped air during welding.
  Samples 2 & 3: No detectable defects.
  Visuals: 3D renderings and defect snapshots along XYZ planes.
 | Sample 1 (DECA 12-CS1) | Sample 2 (SEC 12-SS1) | Sample 3 (PENTA 12-SS1)
Length (mm) | 34.9 | 42.4 | 19.2
Diameter (mm) | 20.5 | 15.2 | 15.6
Material | Carbon Steel 1008 | Stainless Steel 304 | Stainless Steel 304
Source of Welding | In house welding | IMS Engineered Products | IMS Engineered Products
Properties of Weld Samples

## Slide 48
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Geometry | Thickness (mm) | Diameter (in) | Material
Octagon | 1 | 12 | SS 304
Octagon | 2 | 12 | SS 304
SEC | 1 | 18 | CRS 1008
SEC | 2 | 18 | CRS 1008
Pentagon | 1 | 6 | SS 304
Strength Testing
Objective
Determine maximum load capacity and reinflation reliability of modules.
Setup
Modules: See Table.
Technology: Universal Testing Machine (UTM)
Method
Inflate modules.
Compress while depressurized.
Reinflate modules.
Compress until failure.
Figure – Compression of METALS Module.
Table – Summary of Strength-Tested Modules.

## Slide 49
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Max Load Capacity
Material: SS > CRS
Geometry & Thickness: 2mm thickness exceeded 4,000 lbf.
Diameter: larger diameter achieved higher load capacities.
Results
Strength: 2mm thickness ↑ load capacity.
Reusability: Reinflation feasible, minor fatigue over cycles.
Conclusion
Reinflation & Post-Inflation Load
Cycles: 6” pentagon reinflated with slight height/load increases.
Durability: Minor weakening from cracks/voids
Pressure vs Height: Slower expansion at higher pressures
Maximum Loads of 12’’ SS OCT and 18’’ CRS SEC with Different Thickness.
Strength Testing

## Slide 50
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Max Load Capacity
Material: SS > CRS
Geometry & Thickness: 2mm thickness exceeded 4,000 lbf.
Diameter: larger diameter achieved higher load capacities.
Results
Strength: 2mm thickness ↑ load capacity.
Reusability: Reinflation feasible, minor fatigue over cycles.
Conclusion
Reinflation & Post-Inflation Load
Cycles: 6” pentagon reinflated with slight height/load increases.
Durability: Minor weakening from cracks/voids
Pressure vs Height: Slower expansion at higher pressures
Top – Re-Inflation Heights of SS 6’’ Pentagon Modules.
Bottom – Maximum Loads of SS 6’’ Pentagon Modules.
Strength Testing

## Slide 51
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
  Reliability and Scale Tests
  Quality Control Checks
  Performance of Larger and Thicker Modules
  Lunar Welding
  Repairability of METALS on Lunar Surface
  Thermal Management and Cryogenics​
  Heat Transfer Reduction Methods​
  Optimization of Thermal Management​
  Installation​
  Excavation and Installation​
  Integration with Artemis Base
  Geometry Optimization​​
  Custom Pipe Fittings​
Path-To-Flight

## Slide 52
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Scalability to Lunar Use Case
  SEC modules displayed self-similarity in shape once their inflation “plateau” was reached, with
    No significant dependence on sheet metal material and thickness
  SEC Inflation demonstrated pressurization up to 54% of material limit
    Estimated by spherical hoop stress,
  Extrapolate to larger diameters to estimate scalability of storage capacity
At of storage per of sheet metal, one Starship HLS can carry enough METALS for the capacity of 5

## Slide 53
Demonstrated affordable, accessible, and reliable processes for manufacturing and repair
Optimized Sinusoidal Edge Curve (SEC) design maximizes deployed volume and working pressure
Successfully demonstrated scalability up to 48” diameter, creating pathway to scale for Artemis-relevant storage capacities
Key Accomplishments
METALS is a high-value, low-risk, low-cost inflatable solution for scalable, sustainable lunar infrastructure within the decade
Design performance assessed under lunar conditions of vacuum and cryogenic temperatures

## Slide 54
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
References & Acknowledgments
S. Mustafi, E. R. Canavan, R. F. Boyle, J. S. Panek, S. M. Riall, and F. K. Miller, “Active Co-storage of cryogenic propellants for lunar exploration,” NASA NTRS 20080039164, 2008.
B. C. Buckles, J. M. Schuler, A. J. Nick, J. D. Smith, and T. J. Muller, “ISRU Pilot Excavator - development of autonomous excavation algorithms,” in Space Resources Roundtable, XXII Meeting, 2022.
R. B. Malla and K. M. Brown, “Determination of temperature variation on lunar surface and subsurface for habitat analysis and design,” Acta Astronaut., vol. 107, pp. 196–207, 2015.
G. Sanders and J. Kleinhenz, “In Situ Resource Utilization (ISRU) Envisioned Future Priorities,” Nasa.gov. [Online]. Available: https://www.nasa.gov/wp-content/uploads/2023/06/live-isru-efp-new-3-21-23-tagged-1.pdf.
S. Mustafi, E. Canavan, R. Boyle, J. Panek, and S. Riall, “Active Co-Storage of Cryogenic Propellants for Lunar Explortation,” Nasa.gov. [Online]. Available: https://ntrs.nasa.gov/api/citations/20210024522/downloads/SLS-SPEC-159%20Cross-Program%20Design%20Specification%20for%20Natural%20Environments%20(DSNE)%20REVISION%20I.pdf. [Accessed: 17-Oct-2024].
R. Lawler, “SpaceX’s plan for in-orbit Starship refueling: a second Starship,” Engadget, 29-Sep-2019. [Online]. Available: https://www.engadget.com/2019-09-28-starship-refueling-spacex.html.
B. Ridgeway, “Fission Surface Power,” NASA, 09-May-2023. [Online]. Available: https://www.nasa.gov/tdm/fission-surface-power/.
L. Hall, “Lunar south pole oxygen pipeline,” NASA, 09-Jan-2023.
X. Xiao, S. Yu, J. Huang, H. Zhang, Y. Zhang, and L. Xiao, “Thermophysical properties of the regolith on the lunar far side revealed by the in situ temperature probing of the Chang’E-4 mission,” Natl. Sci. Rev., vol. 9, no. 11, p. nwac175, 2022.

## Slide 55
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Thank you!

## Slide 56
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Appendix Slide: Heat Transfer Reduction Methods
  Outside PSR (Heat Reduction)
    Regolith Burying
    Shading
    Reflective Coatings
    Combination of 1, 2, and/or 3
  Within PSR (Heat Induction)
    Heating Device
    Thermal Pathways
    Combination of 1 and/or 2
  Alternatives
    Solid-State Storage (PSR)

## Slide 57
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
  Data Collection
    Data Statistics: 5,991 slice images (1,997 per sample) compiled into 3D renderings.
    Scanning Statistics: Using the SkyScan 1276 microCT, all samples were scanned at 6 µm resolution through full 360° rotation. The Amira software from Thermo Fisher Scientific (formerly FEI) enabled defect isolation, dataset alignment, and 3D visualization.
Appendix Slide: Reliability of Welds – Imaging Parameters
Voxel Size (µm) | Voltage and Current (kV, µA) | Filters | Exposure (ms) | Averages per Projection | Pixel Binning | Scan Time (minutes)
18.5 | 100, 200 | Al+Cu | 230 | 2 | 2x2 | 30
Table 8: SkyScan 1276 Micro-Computed Tomography X-Ray Parameters

## Slide 58
Northwestern University | METALS: Metallic Expandable Technology for Artemis Lunar Structures
Appendix Slide: Storage Temperatures/Pressures Required